|  | EUROPEAN COMMISSION RESEARCH DIRECTORATE-GENERAL Marie Curie Actions – Fellowships | EIF-OIF-IIF-IRG-ERG Final Activity and Management Report |
| --- | --- | --- |

Project no: 225589

Project Acronym: MECOFUPO

Project Full Name: Metal-containing Functional Polymers through Subcomponent Self-Assembly

Marie Curie Actions

EIF-OIF-IIF Midterm review Activity and Management Report

Period covered: from 01-05-2009 to 30-04-2011

Period number:

Start date of project: 01-05-2009

Project coordinator name: Dr Jonathan R. Nitschke

Project coordinator organisation name: The Chancellor, Masters and Scholars of the University of Cambridge

Date of preparation: 01-04-2011

Date of submission (SESAM): 30-04-2011

Duration: 24 Months

Version: 1

- Final publishable summary report

Part I. We have developed a new kind of material using the techniques of subcomponent self-assembly. The condensation of linear diamines and dialdehydes around copper(I) templates in the presence of bulky trioctylphosphine ancillary ligands gave a linear, conjugated polymeric material in DMSO solution.

Scheme 1. Preparation of copper containing polymer 1 via subcomponent self-assembly (left), cartoon representation of 1  (middle). CAChe MM2 minimized structure of an octameric oligomer of 1 (right).

This new, unprecedented material has been characterized by NMR (1H, 13C, 19F, 31P), mass spectrometry, viscometry, micro-rheology, imaging techniques (SEM, AFM, EDX), UV, Photoluminescence and conductivity

This polymer solution was observed to undergo sol-to-gel transition as the temperature was raised to 140°C, in contrast with the behavior of most gel-forming polymers, which do so upon cooling. We attribute the sol-to-gel transition to the formation of CuIN4 crosslinks as the equilibria 2[CuIN2P2] ← [CuIN4] + [CuPn]+ + 4-n P favor the right-hand side at higher temperatures. The material was also observed to exhibit thermochromism and photoluminescence, with the color and intensity of both absorption and emission exhibiting temperature dependence. This material thus responds predictably to combinations of stimuli (heat, light, mechanical shear) in an interconnected way, as is required to generate complex function. In addition, the viscoelasticity of the gel shows an unexpected two steps process gelation.

Part II. Motivated by the results obtained for the first generation of polymer we have pursued to build a different kind of polymer based on double helicate architecture. The molecule synthesized based on the design shown on scheme 2 are thought to act as molecular copper wire as shown in previous work.

2

Scheme 2. Preparation of copper containing double helical polymer 2 via subcomponent self-assembly (left).  CAChe MM2 minimized structure of a hexadecameric oligomer of 2 (right).

The material obtained was characterized by all standards techniques. Results obtained in particles characterization showed aggregation into larger structures either once deposited on a silicon surface or in solution. This suggests the feasibility of growing larger molecule with this type of system. Preliminary results obtained on conductivity and electrochemistry show that the molecule is electro active, therefore suggesting its potential use in electrochemical devices.

This type of material is thought to find applications in nano-electronic. Different collaborations have been set between three departments at the University of Cambridge in order to study the properties of this new, unprecedented material.

CAChe WorkSystem v. 6.1.12.33; Fujitsu Limited: 2007

Schultz, D.; Biaso, F.; Shahi, A. R. M.; Geoffroy, M.; Rissanen, K.; Gagliardi, L.; Cramer, C. J.; Nitschke, J. R. Chem. Eur. J. 2008, 14, 7180.